## Slide 1: Iron nanomaterials in decontamination technologies and their interactions with microorganisms
RNDr. Jaroslav Semerád, Ph.D.

## Slide 2: Worldwide contamination
Persistent organic pollutants (POPs) are organic compounds that are resistant to environmental degradation through chemical, biological, and photolytic processes.
Because of their persistence, POPs bioaccumulate with potential adverse impacts on human health and the environment.

## Slide 3: Decontamination technologies
Thermal desorption
Excavation or dredging
Surfactant enhanced aquifer remediation (SEAR)
Pump and treat
Solidification and stabilization
In situ oxidation
Soil vapor extraction
Nanoremediation
Bioremediation
Collapsing air microbubblesediation (SEAR)

## Slide 4: Decontamination technologies
Bioremediation
Nanoremediation
Nanobioremediation

## Slide 5: nanoscale Zero-Valent Iron (nZVI)
Fe0 + oxidized X  Fe2++ reduced X
2 Fe0 + 2 H2O + O2  2 Fe2+ + 4 OH−
Fe0 + 2 H2O  Fe2+ + H2 + 2 OH−
Natural oxidation of Fe0 in water under aerobic and anaerobic condition:
Fe0
Cr(VI) REDUCTION BY nZVI

## Slide 6
Fe0
Soil and groundwater clean-up
Waste water treatment
Oxidation of nZVI - aging
Fe0
Complete oxidation
Interaction of nZVI with microorganisms
Semerád, J, & Cajthaml, T 2016, 'Ecotoxicity and environmental safety related to nano-scale zerovalent iron remediation applications', Applied Microbiology And Biotechnology. ISSN: 1432-0614
Time
Real concentrations used in practice (up to 10 g/L)

## Slide 7
Phase I: In-situ chemical reduction by nZVI (2 injection campaigns 20 kg nZVI each by direct push)
Phase II: Bioreduction stimulated by organic substrate (8 m3 of whey)
MV-4
MV-3
MV-2
IN-2
IN-1
MV-1
HS-1
GW flow
Combined Nano-Biotechnology for In-Situ Remediation of Mixed Contamination of Groundwater by Hexavalent Chromium and Chlorinated Solvents

## Slide 8
MICROBIOLOGICAL REDUCTION OF Cr(VI)
Aerobic reduction:
electron donor (reduced) + Cr(VI) (electron acceptor oxidized) + oxygen +bacteria = Cr(III)(electron acceptor reduced) + CO2(electron donor oxidized) + H2O
Anaerobic respiration:
electron donor (reduced) + Cr(VI) (electron acceptor oxidized) + bacteria = Cr(III)(electron acceptor reduced) + CO2(electron donor oxidized) + CH4
Electron donors: „natural“ organic substrates (humic and fulvic acids) or „artificial“ (e.g. ethanol, glucose, whey, glycerol, lactate, butyrate,...)
Indirect reduction:
Cr(VI) by Fe(II) or H2S, originating by metabolism of iron reducing bacteria (IRB) and sulfate reducing bacteria (SRB)

## Slide 9
β-elimination
hydrogenolysis pathway
CHCl=CCl2 + 2e-→ HC≡CCl + 2Cl-
CH2=CCl2 + 2e- + H+→ CH2=CHCl + 2Cl-
Pathways of abio- and bio- reduction of chlorinated ethenes
Combined Nano-Biotechnology for In-Situ Remediation of Mixed Contamination of Groundwater by Hexavalent Chromium and Chlorinated Solvents

## Slide 10
Combined Nano-Biotechnology for In-Situ Remediation of Mixed Contamination of Groundwater by Hexavalent Chromium and Chlorinated Solvents
Hydrogeological settings:
Quaternary aquifer (clayey gravel)
Saturated thickness 3.5 m
Cr(VI) concentration in groundwater
up to 50 mg/l
cVOCs concentration in groundwater
up to 6500 µg/l (TCE dominates)
TDS 800 – 900 g/l
Eh 300 - 440 mV
pH 7 – 7.2

## Slide 11
Cr(VI)
Combined Nano-Biotechnology for In-Situ Remediation of Mixed Contamination of Groundwater by Hexavalent Chromium and Chlorinated Solvents

## Slide 12
CVOCs
Combined Nano-Biotechnology for In-Situ Remediation of Mixed Contamination of Groundwater by Hexavalent Chromium and Chlorinated Solvents

## Slide 13
Cr(VI) chlorine number
Combined Nano-Biotechnology for In-Situ Remediation of Mixed Contamination of Groundwater by Hexavalent Chromium and Chlorinated Solvents

## Slide 14
Molecular biology methods
Nanofiber carriers
Monitoring well
Detection of Dehalobacter , Dehalococcoides and Sulfurospirillium by PCR or qPCR
Presence of funcional genes (bvcA and vcrA) by qPCR
Total biomass quantified by qPCR using 16SrRNA and PLFA
Illumina MiSeq amplicon sequencing
Combined Nano-Biotechnology for In-Situ Remediation of Mixed Contamination of Groundwater by Hexavalent Chromium and Chlorinated Solvents

## Slide 15
Molecular biology methods Transformation product analysis

## Slide 16
Němeček J., Pokorný P., Lhotský O., Knytl V., Najmanová P., Steinová P., Černík M., Filipová A., Cajthaml T. Science of the Total Environment, doi:10.1016/j.scitotenv.2016.01.019.
Combination of nano-bio reduction exhibited high efficiency of Cr(VI) and cVOC removal
The results indicates a reciprocal effect of both the abiotic and the biotic processes: reduction of Cr(VI) by reductants (mainly FeII) produced or recycled by microbial processes
cVOCs were removed by chlororespiring community developed subsequently

## Slide 17: The effect of nZVI on resident microbial population from a real contaminated site
200 L of real contaminated water from Spolchemie company (Czech Republic)
Main contamination by chlorinated solvents
2 months of exposition with Biochar and a composite Biochar-nZVI material (0.7 g/L)
After 1 week, the addition of whey (170 mg/L)
Closed system, 14 ± 2 °C

## Slide 18: Evolution of nZVI-based material during the aging
Chart: Dissolved iron (Fe2+)
| T0 | T3 | T7 | T14 | T30 | T60
Control | 1.9348 | 4.4315 | 1.6529 | 1.3179 | 1.2178 | 0.7688
Biochar | 1.9348 | 4.7433 | 2.0173 | 1.3154 | 1.1858 | 0.8481
Biochar-nZVI | 1.9348 | 14.7011 | 34.0716 | 57.9989 | 16.2458 | 17.0268
Chart: pH
| T0 | T3 | T7 | T14 | T30 | T60
Control | 6.475 | 6.4487 | 6.4857 | 6.5133 | 6.6397 | 6.742
Biochar | 6.475 | 6.459 | 6.522 | 6.5757 | 6.6887 | 6.9177
Biochar-nZVI | 6.475 | 6.5677 | 6.7833 | 7.1337 | 7.2877 | 7.3213
Chart: ORP
| T0 | T3 | T7 | T14 | T30 | T60
Control | 48.85 | 53.6667 | 78.5667 | 249.4667 | 251.2667 | -40.7667
Biochar | 48.85 | 44.3333 | 116.3667 | 107 | 20.1667 | -31
Biochar-nZVI | 48.85 | -68 | -87.2 | -329.2667 | -136.3333 | -156

## Slide 19: The effect on microbial communities of the contaminated site
1) qPCR
2) NGS

## Slide 20: The effect on microbial communities of the contaminated site - with the incorporation of a biostimulation step
1) Total organic carbon
2) Microbial biomass estimated by phospholipid fatty acid analysis
Whey application
Whey application

## Slide 21: The effect on microbial communities of the contaminated site - with the incorporation of a biostimulation step
3) qPCR
4) NGS

## Slide 22: Risk assesment questions
Toxicity of nanoparticles - how to measure toxicity of nZVI?
The evolution of toxicity?
Are the oxidation products of nZVI more or less toxic?

## Slide 23: Oxidative damage of biomolecules caused by ROS
Fe0
1.
3.
2.
Glyoxale
Formaldehyde
Acroleine
Methylglyoxale
Oxidized bases
8-hydroxy-2'-deoxyguanosine
Methionale
Benzaldehyde
Formaldehyde
Malondialdehyde
Methacroleine
Semerád, J, & Cajthaml, T 2016, 'Ecotoxicity and environmental safety related to nano-scale zerovalent iron remediation applications', Applied Microbiology And Biotechnology. ISSN: 1432-0614
Cell-nanoparticle interactions
Fe0 + O2 + 2 H+  Fe2+ + H2O2
Fe0 + H2O2  Fe2+ + 2 OH−
Fe2+ + H2O2  Fe3+ + OH• + OH−
Fe3+ + H2O2  Fe2+ + OOH− + H+  Fe2+ + 2 H+ + 2 O2−

## Slide 24: Markers of protein and lipid oxidation
Screening for new markers of oxidative stres damage was done using HS-SPME-GC-MS.
Two markers of protein oxidative damage were found in yeast and bacteria species.
Several other markers of lipid peroxidation were found in all microorganisms tested.
Aldehyde quantification could serve as a way of evaluating oxidative stress in environmental samples from sites of nZVI injection.
Fungi
Algae
Bacteria
Saccharomyces cerevisiae BY 4742
Desmodesmus subspicatus CCALA 688
Bacillus cereus DB 3035
Serratia marcescens CCM 303
Semerád et al. 2019 ‘Oxidative stress in microbes after exposure to iron nanoparticles: Analysis of aldehydes as oxidative damage products of lipids and proteins‘. Environmental Science and Pollution Research. In press.

## Slide 25: Markers of protein and lipid oxidation
Bacteria
Bacillus cereus DB 3035
Serratia marcescens CCM 303
Fungi
Saccharomyces cerevisiae BY 4742
Lipid peroxidation products
Products of protein oxidation
Glyoxale
Methionale
Benzaldehyde
Formaldehyde
Acrolein
Methylglyoxale
Methacrolein
Semerád et al. 2019 ‘Oxidative stress in microbes after exposure to iron nanoparticles: Analysis of aldehydes as oxidative damage products of lipids and proteins‘. Environmental Science and Pollution Research. In press.

## Slide 26: Quantification of malondialdehyde – a novel approach for toxicity testing of nZVI-based nanomaterials
1) Cultivation of tested bacteria
2) Preconcentration of bacterial suspension
3) Cell counting by flow cytometry
4) Exposition with iron nanoparticles
5) Reaction with thiobarbituric acid
6) Extraction of MDA-TBA complex
7) Quantification by RP-HPLC-FLD method

## Slide 27: Application of MDA assay to determine acute toxicity of newly developed nZVI-based nanoparticles
Pseudomonas putida CCM
 | EC50 [g/L] | EC50corrected [g/L]
nZVI | 0.5 | 0.5
S-nZVI 0,25% | 0.5 | 0.6
S-nZVI 1% | 0.4 | 1.0
S-nZVI 5% | 0.4 | 5.7
Semerád et al. 2019, Environmental fate of sulfidated nZVI particles: interplay of nanoparticle corrosion and toxicity during the aging

## Slide 28
Fe0
Fe0
Aging of nanoparticles during 60 days
Fe0
FeOx
Day 0
Day 60

## Slide 29
Fe0
Fe0
Aging of nanoparticles during 60 days
Fe0
FeOx

## Slide 30: Conclusions
nZVI cause oxidation to biomolecules in microbes
Toxicity of nZVI rapidely decrease during the time
nZVI decrease level of contamination and overall toxicity
Recent results proves a reciprocal effect of both the abiotic and the biotic processes: reduction of contaminants by reductants (mainly FeII+) produced or recycled by microbial processes

## Slide 31
Thank you for your attention